Temperature and illumination dependent mass transport

during the surface relief formation in As-S(Se)  amorphous chalcogenides

Sandor Molnar1*, Roland Bohdan1, Viktor Takacs2, Istvan Csarnovics1,

Yuri Kaganovsky3, Sandor Kokenyesi1

1 Institute of Physics, Faculty of Science and Technology, University of Debrecen,

Egyetem sq.1, Debrecen, 4032, Hungary

2Institute of Nuclear Research, Hungarian Academy of Sciences,

Debrecen, Bem sq.18/c, 4026, Hungary

3 Department of Physics, Bar-Ilan University, Ramat-Gan 52900, Israel

Investigations of amplitude-phase optical and geometrical relief formations at room temperatures, rather well known for a-Se and selected compositions from As-Se system [1,2], were extended towards wide temperature range from 77 K up to softening temperatures of given materials. Besides the holographic recording of periodical 1D or 2D surface relief structures experimental techniques were developed and used for in-situ or afterwards measurements of complementary changes in optical transmission and surface relieves. It was shown that changes of optical density and surface relieves can be detected at temperatures down to liquid nitrogen and up to softening temperatures of the given glass compositions. The rate of the processes increases with temperature following Arrhenius law with rather small activation energies, but at temperatures close to the softening temperature thermal erasing prevails. The possible role of diffusion, related to different components of glass and viscosity in these light and temperature stimulated mass transport processes was analyzed. This way the interrelations between composition, recording conditions and efficiency, erasing processes and stability were established for samples from the given system of materials.

Acknowledgement

Authors  acknowledge the support of the  GINOP-2.3.2-15-2016-00041 project .

References

[1] Kaganovskii, Yu., Trunov, M.L., Beke, D.L., Kökényesi, S. Mechanism of photo induced mass transfer in amorphous chalcogenide films, Materials Letters, 66 (1) ,  159-161 (2012).

[2] Bohdan, R.,  Molnar, S. ,  Kokenyesi, S., Methods comparing peculiarities of surface-relief recording in amorphous chalcogenides  , Physica Status Solidi (A) Applications and Materials Science , 212, Iss. 10,  2186-2190 (2015).