Spin-coated As30Se70 chalcogenide glass thin films – novel approach for solvent formulation

Stanislav Slang1\*, Petr Janicek2,1, Karel Palka3,1, Miroslav Vlcek1

1Center of Materials and Nanotechnologies, Faculty of Chemical Technology, University of Pardubice, Studentska 95, Pardubice 532 10, Czech Republic

2Institute of Applied Physics and Mathematics, Faculty of Chemical Technology, University of Pardubice, Studentska 95, Pardubice 532 10, Czech Republic

3Department of General and Inorganic Chemistry, Faculty of Chemical Technology, University of Pardubice, Studentska 95, Pardubice 532 10, Czech Republic

\*presenting author

Chalcogenide glasses (ChGs) are semiconducting materials with high refractive index and wide IR transmission window. Due to their unique properties, they have found many applications in optics, optoelectronics and photonics. ChGs can be used in a form of bulk material, fibers or as a thin film deposited on appropriate substrate. The thin films are frequently deposited by physical vapor deposition techniques (e.g. thermal evaporation, laser ablation, etc.) but solution based techniques (e.g. spin-coating, dip-coating, spiral bar-coating, etc. [1]) which exploit solubility of ChGs in volatile alkaline amines are also gaining attention. The main advantage of solution based deposition techniques lies in low cost instrumentation, simplicity of thin films deposition and ability to use flexible substrates. However, poor solubility of selenide ChGs in volatile amine solvents limits the variety of glass compositions suitable for solution processing.

Previously, the arsenic-selenide thin films were deposited from ethylenediamine [2] or ethanolamine [3] solutions but their optical quality, roughness or targeted composition were highly affected. Also, the high boiling points and low volatility of used solvents dampened the possibility of successful organic residuals removal from deposited thin films.

In this work, we present the study of volatile amine-based solvent formulation and its influence on As30Se70 ChG solubility and dissolution mechanism. The stable solutions of quantitatively dissolved selenide ChG were used for spin-coating of thin films in specular optical quality. The post-deposition thermal treatment proved to have high impact on thickness, optical properties and structure of studied thin films. The content of organic residuals was also significantly reduced. The proper solvent formulation and thermal stabilization process yielded the thin film with high refractive index, very low surface roughness and composition close to the source bulk glass.

**References**

[1] S. Slang, P. Janicek, K. Palka, M. Vlcek, Opt. Mater. Express 6 (2016) 1973-1985.

[2] Y. Zou, H. Lin, O. Ogbuu, L. Lin, S. Danto, S. Novak, J. Wilkinson, J. D. Musgraves, K. Richardson, J. Hu, Opt. Mater. Express 2 (2012) 1723–1732.

[3] Prince, R. Singh, M. Zulfequar, A. Kumar, P. K. Dwivedi, J. Non-Cryst. Solids 476 (2017) 46-51.

**Acknowledgements**

Authors appreciate financial support from project No. 16-13876S financed by the Grant Agency of the Czech Republic (GA CR), support from the grants LM2015082 and ED4.100/11.0251 from the Ministry of Education, Youth and Sports of the Czech Republic and European Regional Development Fund-Project "Modernization and upgrade of the CEMNAT" (No. CZ.02.1.01/0.0/0.0/16\_013/0001829).

Preferred presentation form: **POSTER**